Technical Characteristics

|  |  |  |
| --- | --- | --- |
| Name of the indicator  | Crystalline (sintered) | Polycrystalline |
| Chemical formula | B | B |
| Appearance | a piece(powder) | powder |
| Mass fraction % |  |  |
| BOR, not less than | 96,0 | 94,0 |
| Magnesium | - | 0,5 |
| Iron (Fe), not less than | 0,5 | 0,3 |
| Carbon (С), not less than | 2,0 | 3,0 |
| Dispersion, mm | 2-50 | 0,063-0,30 |
| \* It is possible to change the indicator in agreement with a customer (for all brands) |  |  |